Electrochemical Nitrogen Reduction to Ammonia with Mesoporous Molybdenum-Carbon Electrocatalysts in a Gas Diffusion Flow Cell

Chaoyun Tang,1+ Dipankar Saha,2+ Jiacheng Wang,1 Arvind Chandrasekar,3 Negar Sabouhanian,4 Connor L. Witt,2 Yulei Wang,1 Aicheng Chen,4 Wei Fan,1 Chung-Li Dong, 3 Zhu Chen,1 James J. Watkins,2* and Nianqiang Wu1*

1Department of Chemical and Biomolecular Engineering, University of Massachusetts, Amherst, MA 01002, United States

2Conte Center for Polymer Research, Department of Polymer Science and Engineering, University of Massachusetts, Amherst, MA 01002, United States

3Department of Physics, Tamkang University, New Taipei City, Taiwan

4Department of Chemistry, University of Guelph, Guelph, Canada

*Corresponding author’s email:

nianqiangwu@umass.edu and watkins@umass.edu

+ Equal Contribution

ABSTRACT

Electrochemical nitrogen reduction (eNRR) is limited by the availability of efficient catalysts, scalable flow-cell architectures, and understanding of performance-limiting processes. This work addresses these issues through systematic catalyst-device-mechanism study. First, molybdenum (Mo) single-atoms and nanoparticles supported on mesoporous nitrogen-doped carbon are synthesized with tunable pore sizes using a five-second photothermal pyrolysis of a self-assembled bottlebrush block copolymer (BBCP) template. Atomic dispersion of Mo maximizes electrochemically accessible active surface area and enhances intrinsic reaction kinetics. Second, a gas diffusion electrode (GDE) flow cell is constructed to evaluate catalyst performance under continuous operation. The optimized catalyst-device system achieves a Faradaic efficiency of 21.6% and an ammonia yield rate of 34.7 μg h⁻¹ mg⁻¹, with intermediate pore sizes and balanced electrode wettability enabling effective triple-phase boundary formation and active-site utilization. Third, electrochemical characterization was combined with an exploratory machine learning analysis of 23 flow cell records. The models describe associations between four controlled variables and the measured performance within the sampled ranges. Mo content had the largest SHAP contribution for both targets. Pore size, catalyst loading, and electrode wettability showed different associations for the two targets. Because the dataset is small and was not independently validated, these results are descriptive and should not be treated as universal design principles. This study provides a unified framework linking catalyst structure, electrode architecture, and kinetic limitations in eNRR flow-cell systems.

Keywords: electrochemical nitrogen reduction, molybdenum single atoms, gas diffusion electrode, machine learning, bottlebrush block copolymer templates.

INTRODUCTION

Ammonia serves as clean fuels, industrial feedstock and especially fertilizers that sustain global food production.  About 183 million tons of ammonia are produced globally every year,1  and over 90% of ammonia is produced via the Haber-Bosch process, which operates at high temperatures and pressures and consumes 1-3% of global energy while emitting more than 300 million tons of CO2 annually.2,3These drawbacks highlight the need for sustainable, low-carbon nitrogen fixation technologies. Electrochemical nitrogen reduction (eNRR) is a promising alternative, enabling ammonia synthesis under ambient conditions using renewable electricity and offering the potential for decentralized production.4, 5 Despite extensive catalyst development, eNRR remains far from industrial viability, with low ammonia yield rates (≈6120 μg h-1 cm-2), limited Faradaic efficiencies (<30%), and persistent challenges including low N2 solubility, sluggish N≡N activation, competition from hydrogen evolution, and incomplete mechanistic understanding.6, 7

Inspired by the active sites of nitrogenase enzymes in biological nitrogen fixation, Mo has emerged as a highly promising catalytic center for eNRR.8 Density functional theory studies and bioinspired design principles have shown that Mo can effectively adsorb N2 and stabilize key intermediates, which are critical for selective NH3 formation.9, 10 While these insights provide a strong theoretical foundation for Mo-based catalyst development, current systems face several limitations that hinder practical application. For example, several Mo-based eNRR catalysts are based on oxide-derived Mo species on low-surface-area carbon supports, which primarily limits the density and accessibility of electrochemically active sites, rather than uniformly controlling metal dispersion.11, 12 In addition, the electronic and geometric configuration of Mo centers is typically poorly controlled, which reduces both selectivity and intrinsic activity. Traditional H-type electrochemical cells further restrict gas transport and triple-phase boundary formation, making kinetic analysis challenging.5, 13 Moreover, despite advances in materials design, establishing clear correlations between catalyst structure and electrochemical performance, especially under high-current-density conditions relevant for practical ammonia production, remains difficult. Collectively, these limitations highlight a critical need for strategies that enhance mass transport, maximize active-site utilization, and elucidate mechanistic pathways, while simultaneously improving ammonia yield and Faradaic efficiency.

Considering  low-solubility gaseous reagents for eNRR and drawing inspiration from other electrochemical reactions such as electrochemical CO2 reduction,14, 15 we identified two key strategies to advance the field: (i) the creation of high surface-area porous supports to maximize catalyst exposure and to increase mass loading of the electrode, and (ii) the integration of catalysts into electrode architectures that facilitate gas transport and triple-phase boundary formation. Guided by these principles, we developed a rapid, tunable strategy to synthesize porous metal-based carbon materials using bottlebrush block copolymers (BBCPs).16-18 This approach allows precise control over pore architecture, and when combined with ultrafast photothermal pyrolysis,19 mesoporous carbon films can be formed within seconds. A critical advantage of this method is its flexibility: metals, including Mo, can be incorporated in various sizes, enabling the formation of single atoms, sub-nanometer clusters, or nanoparticles, with controlled coordination environments. This capability directly addresses a major limitation of prior Mo-based catalysts by providing well-dispersed, structurally defined active sites that are fully electrochemically accessible. To further tackle limitations associated with diffusion and device-level evaluation, we integrated these Mo-C porous catalysts into an electrochemical flow cell equipped with a GDE. In this configuration, N2 is delivered directly to the catalyst, stabilizing the triple-phase boundary and minimizing mass-transport limitations, which enables continuous operation under high-current-density conditions. By combining advanced catalyst design with optimized device architecture, this platform provides a realistic assessment of intrinsic catalytic activity and a route toward practical eNRR implementation.

In this work, the nitrogen-doped carbon catalysts are tailored with pore size ranging from 10 to 56 nanometers, anchored with Mo single metal atoms and small nanoparticles. This approach overcomes limitations related to uncontrolled metal dispersion and poorly defined coordination environments while enhancing mass transport. The combination of BBCP templates and ultrafast photothermal pyrolysis enables precise control over pore architecture, high molybdenum dispersion, and maximized active-site exposure, ensuring full utilization of intrinsic catalytic activity. Characterization using X-ray absorption near-edge structure (XANES), extended X-ray absorption fine structure (EXAFS), and X-ray photoelectron spectroscopy (XPS) provides detailed insights into the chemical states and local coordination environment of molybdenum with nitrogen and oxygen, revealing how the arrangement and interaction of metal atoms are established and stabilized during the synthesis process. Building on this materials platform, the catalysts are integrated into a GDE flow cell, which enhances nitrogen delivery, stabilizes the triple-phase boundary, and mitigates the low solubility of nitrogen in aqueous electrolytes, which is critical for achieving high reaction rates. The flow-cell design also supports continuous operation at high current densities and facilitates scalable ammonia production, while the use of solid polymer electrolytes simplifies device architecture and improves experimental reliability. To understand the relationships between catalyst structure and performance, we combine systematic electrochemical testing with machine learning-assisted analysis to identify the parameters that strongly influence Faradaic efficiency and ammonia yield, establishing quantitative correlations between structure, function, and device performance. By addressing fundamental limitations in catalyst design, device architecture, and reaction mechanisms, this work establishes a generalizable framework for efficient ambient ammonia synthesis and the rational development of next-generation nitrogen reduction systems.

EXPERIMENTAL SECTION

Materials

All materials were used without further purification unless otherwise noted. The following compounds were obtained from Sigma-Aldrich: cis-5-norbornene-exo-2,3-dicarboxylic anhydride, N,N′-dicyclohexylcarbodiimide (DCC, >99%), dopamine hydrochloride, ammonium molybdate tetrahydrate, 4-dimethylaminopyridine (DMAP, >99%), and 5-norbornene-2-endo,3-exodicarboxylic acid (97%). Ethyl vinyl ether (>99%), magnesium sulfate (∼99.5%), ammonia solution (28–30%), anhydrous dimethylformamide (DMF, ∼99.8%), anhydrous dichloromethane (DCM, ~99.8%), and tetrahydrofuran (∼98%) were also sourced from Sigma-Aldrich. Poly(ethylene glycol) monomethyl ether poly(styrene) (∼99%, Mw = 5 kg∙mol–1) and poly(styrene)-b-poly(ethylene oxide) were provided by Polymer Source. Anhydrous ethanol was acquired from Fisher Scientific. Third-generation Grubb’s catalyst (G3) was synthesized following established procedures. Silicon wafers were purchased from University Wafer, Inc. (Boston, MA, USA). Ultrapure type I water (18.2 MΩ·cm) was used for all experiments.

Synthesis of Polystyrene-block-Poly(ethylene oxide) Bottlebrush Block Copolymers (PS-b-PEO BBCP)

Norbornene-capped polystyrene (PS-NB, Mw = 5 kg∙mol-1) and polyethylene oxide (PEO-NB, Mw = 5 kg∙mol-1) macromonomers were synthesized following a previously reported method. To prepare the PS-NB macromonomer, 2 g of hydroxyl-terminated polystyrene (PS-OH), 0.27 g of exo-5-norbornenecarboxylic acid, 0.31 g of N,N′-dicyclohexylcarbodiimide (DCC), and 0.03 g of 4-dimethylaminopyridine (DMAP) were added to a dry flask containing 50 mL of anhydrous dichloromethane (DCM). The reaction was conducted at room temperature for 3 days. Upon completion, the product was concentrated using rotary evaporation to remove excess solvent. The resulting mixture was transferred to an extraction funnel with 150 mL of 1 M HCl and NaOH solution, and the bottom layer was collected after three extractions, followed by a rinse with brine. Magnesium sulfate was added to the solution, stirred for 15 minutes, and filtered. The solid byproduct was discarded, and any remaining solvent was removed by rotary evaporation, yielding a viscous solution. This viscous solution was then precipitated dropwise into chilled methanol, resulting in the formation of norbornene-terminated polystyrene (PS-NB), confirmed to have a molecular weight of 5 kg∙mol-1 by GPC. The PEO-NB was synthesized using a similar method and was purified with cold ether.

For the subsequent polymerization, 400 mg of each synthesized macromonomer (PEO-NB and PS-NB) was placed in a reaction vial with DCM under an argon-filled glovebox. The concentrations of PS-NB and PEO-NB were set at 0.5 M and 0.13 M, respectively. The ring-opening metathesis polymerization (ROMP) was initiated with the PEO-NB block using a calculated amount of G3 catalyst for approximately 15 minutes. Following the completion of the PEO block, a solution of PS-NB was added to the reaction mixture. The mixture was allowed to react for an additional 2 hours to ensure complete polymerization, after which the reaction was terminated with 0.2 g of ethyl vinyl ether. The resulting ether-terminated mixture was dried overnight in a fume hood, yielding a light brownish solid as PS-b-PEO block copolymer, which was used without further purification.

Preparation of Molybdenum-Nitrogen Bottlebrush Block Copolymer Precursors

Synthesized PS-b-PEO BBCP was utilized as a template for creating porous carbon spheres, following procedures. 200 mg of dopamine was initially dissolved in an 8 mL mixed solution of ethanol and deionized water in a 4:1 ratio. This solution was then added to 1 mL of tetrahydrofuran (THF) containing 30 mg of PS-b-PEO BBCP and molybdenum salt (depending on the weight percentage) while stirring gently at 900 rpm. After 1 hour, polymerization of the dopamine was initiated by adding 500 μL of an ammonia-aqueous solution, which resulted in a noticeable color change. The reaction vial was sealed with a punctured parafilm and allowed to react for at least 48 hours. Following the reaction, the mixture was centrifuged at 8000 rpm for 10 minutes and rinsed at least five times with a mixed solvent solution to isolate the composite. The resulting product was spread evenly over a silicon wafer and left to dry overnight at room temperature, forming a thin film that was then prepared for carbonization.

Preparation of Porous Mo-N-C Material

The thin film on the silicon wafer was subjected to photothermal pyrolysis using a Novacentric Pulse Forge 1300 xenon flash lamp system (Austin, Texas) under ambient conditions. The sample was placed 10 mm from the lamp during processing. The film received 15 pulses (energy was 2.61 J∙cm-2 per pulse) at a voltage of 500 V, with each pulse lasting 600 μs at a frequency of 1 Hz, effectively converting the precursor into a Mo-N doped porous few-layer graphitic structure. The yield from this process was found to be 40%, as determined by mass measurements taken before and after the treatment.

Microscopy, Spectroscopy, and Surface Area

X-ray diffraction (XRD) measurements were conducted using a Panalytical X-ray diffractometer, which employed Cu Kα radiation (wavelength = 1.5418 Å). Micro-morphology and structure were analyzed using a field-emission scanning electron microscope (FE-SEM) (JEOL 7600F). HAADF-STEM images were acquired using a TFS Spectra Ultra, which is equipped with an ultra-high-resolution, double-corrected HRTEM/STEM system. The instrument was operated at 300 kV for imaging. Nitrogen adsorption/desorption measurements were performed on an Autosorb-1 system at 77 K, following degassing of the sample at 150 °C for 24 hours. The specific surface area was calculated using the Brunauer–Emmett–Teller (BET) method, based on the relative pressure range of 0.1 to 0.2, with a positive C value used for the calculation. It should be noted that the N2 adsorption/desorption isotherm is not suitable for determining pore size distributions beyond the 20 nm range. To estimate the pore size distribution of the electrocatalyst, TEM imaging was employed, and the data were analyzed using ImageJ software. XPS sample powders were pressed into created cups using a zinc-plated stainless washer with a 3 mm opening secured with 3MTM permanent double-sided tape.  A minimum amount of powder was used to fully cover the bottom of the created well and pressed down with clean weighing paper.  When performed correctly, a small layer of powder sticks to the weigh paper, leaving behind a powder surface that has not touched any other surface. XPS experiments were performed using a Physical Electronics VersaProbe III instrument equipped with a monochromatic Al kα x-ray source (hν = 1,486.6 eV) and a concentric hemispherical analyzer. Charge neutralization was performed using both low energy electrons (<5 eV) and argon ions. The binding energy axis was calibrated using sputter cleaned Cu (Cu 2p3/2 = 932.62 eV, Cu 3p3/2 = 75.1 eV) and Au foils (Au 4f7/2 = 83.96 eV). Peaks were charge referenced to sp2 C-Cx band in the Carbon 1s spectra at 284.5 eV for all samples. Measurements were made at a takeoff angle of 45° with respect to the sample surface plane. This resulted in a typical sampling depth of 3-6 nm (95% of the signal originated from this depth or shallower). Quantification was done using instrumental relative sensitivity factors (RSFs) that account for the x-ray cross section and inelastic mean free path of the electrons. The analysis size was ~200 µm in diameter. The Mo K-edge X-ray absorption near-edge structure (XANES) and extended X-ray absorption fine structure (EXAFS) measurements were conducted at beamline TPS 44A at the Taiwan Photon Source, National Synchrotron Radiation Research Center (NSRRC). The beamline provides an energy resolving power of approximately 7,000. Data acquisition was performed is step-scan mode, and the spectra were recorded in fluorescence yield mode using a seven-channel silicon drift detector (SDD), which enhances signal collection and reliability. The data reduction and analysis were carried out using the Demeter software package, with Athena employed for data processing and Artemis for the structural fitting. The spectra were normalized, background-subtracted, and transformed into χ(k) space, with k3-weighting applied. The Fourier transforms were performed over a k-range of ~3–11 Å-1 to obtain the R-space. Structural parameters, including coordination numbers, interatomic distances, and Debye–Waller factors, were derived via nonlinear least-squares fitting using Artemis/FEFF theoretical modelling.

In situ electrochemical FTIR spectroscopic studies were conducted using an FTIR spectrometer (Nexus 8700) equipped with a liquid N2-cooled HgCdTe (MCT) detector. A three-electrode cell with a Hg/HgO (1.0 M KOH) as a reference electrode and Ti/Ta2O5-IrO2 as a counter electrode was utilized. A suspension of the catalyst was drop-casted onto a piece of graphite foil and attached to the bottom of the Ti rod as a holder, serving as the working electrode. The attenuated total internal reflection mode and potential difference technique were employed during the electrochemical reduction of N2. The FTIR experiments were performed in N2 and Ar-saturated 0.1M KOH solutions, and the relative change in reflectivity (∆R/R) as a function of the wavenumber (cm-1) was measured according to the following equation:

∆RR = [RE2-RE1]R(E1)      	(2)

Where R(E1) exhibits the reflection spectrum acquired at the base potential of +0.2 V vs RHE, and R(E2) represents the reflection spectrum obtained at the sample potential from +0.1 V to -0.2 V vs RHE in 0.1 V intervals. At each potential, 64 IR scans were added and averaged with the instrumental resolution of 4 cm-1. For the time-dependent experiment, each spectrum was recorded every 40 s for a total time of 800 s at a constant potential of -0.2 V vs RHE. The final spectra shown were measured by the subtraction of the relative change in reflectivity (∆R/R) in N2-saturated solution from the one obtained in Ar-saturated solution. According to equation 2, the negative-oriented peaks represent the generation of new species, while the positive-oriented peaks correspond to the consumption of species in the electrolyte.

Electrochemical Measurements and Calculations

The initial evaluations of catalysts for eNRR were conducted at room environment on electrochemical workstation (Solartron analytical, AMETEK Scientific instruments) using a three-electrode configured H-type cell. The catholyte and anolyte were separated by proton exchange membrane (PEM, NafionTM 212, THESIX Technology Solutions) or anion exchange membrane (AEM, Sustainion X37-50 Grade T, Dioxide Materials) based on the electrolyte applied. A glass carbon electrode (GCE) was used as supporter for working electrode. For the preparation of working electrode, 2 mg as-synthesized catalysts were dispersed in 353 μL mixed solution. This mixed solution contained 800 μL, 200 μL ethanol and 80 μL 5 wt. % Nafion in ethanol solution. After ultrasonically treated for 30 min to form a homogeneous ink, 5 μL catalyst ink was drop casted on the center of GCE with a catalyst loading amount of ~0.2 mg∙cm−2 and subsequently dried naturally in air. Pt wire and Ag/AgCl (Saturated KCl electrolyte) were used as the counter electrode and reference electrode, respectively. A representative electrolyte of 0.1 M HCl, 0.1 M Na2SO4 and 0.1 M KOH were used for initial evaluation of as-synthesized catalysts. In this work, all measured electrochemical potentials were calibrated to be vs. Reversible Hydrogen Electrode (RHE) by the following equation:

E(vs. RHE) = E(vs. Ag/AgCl) + 0.199 + 0.059 x pH		(1)

where E(vs. RHE) is the converted potential (V) vs. RHE, E (vs. Ag/AgCl) is the experimentally measured potential against Ag/AgCl reference electrode, 0.199 is the value of standard potential for the Ag/AgCl reference electrode (saturated KCl electrolyte) at 25 °C. After purge with Ar gas for 30 mins, 20 times cyclic voltammetry (CV) were first conducted for surface activation and 3 times linear sweep voltammetry (LSV) were then recorded. Same procedure were conducted after switch to N2 for 30 mins.

Preparation of Gas Diffusion Electrode

To prepare the Mo-SAs GDEs, a homogeneous Mo-SAs ink was prepared first. In typical process, 8 mg of Mo-SAs catalyst, 480 μL of 5 wt. % Nafion/Ethanol solution, 40 μL of 1g∙mL-1 PTFE/ethanol as a polymeric binder (PTFE was combined with the Mo-SAs to give the surface of the electrode a hydrophobic component and prevent flooding), and 280 μL ethanol were mixed and sonicated for 20 mins. The ink was subsequently loaded onto GDL (Sigracet 22 BB, Fuel Cell Store, area: 2x2 cm2) by hand-spraying. The GDL was fixed on a heated metal plate and kept at 120 ºC. As a result, the catalyst loading was 2 mg∙cm-2, the Nafion/catalyst ratio is 25 wt. % and the PTFE/catalyst ratio is 5 wt. %. The catalyst loading and surface hydrophilic/hydrophobic property can be further tuned by adjusting the usage of catalyst and PTFE accordingly.

Electrochemical NH3 Synthesis in GDE Flow Cell

The electrochemical N2 reduces was performed in the flow cell consisting of three compartments. A three-electrode system was established in the flow cell connection with the Potentiostat (Interface 1010B, Gamry) as a power supply. The Mo-SAs GDE was employed as cathode with an active geometric area of 1x1 cm2, A 40 wt. % Pt/C coated GDL was used as anode also with an active geometric area of 1x1 cm2 and an Ag/AgCl electrode (0.199 V vs NHE) as reference electrode. The anion exchange membrane (AEM, Sustainion X37-50 Grade T, Dioxide Materials) with an active geometric area of 1x1 cm2 was used as anode. Two peristaltic pump (YZ1515x, LongerPump) was used to apply electrolytes with a constant flow rate of 30 mL∙min-1 through the flow reactor from bottom to top for both cathodic and anodic chamber. The N2 supply was first go through a gas purifier (an oxidizing trap filled with 0.1 M KMnO4 in aqueous 0.1 M KOH) to remove any NOx. Then the gas flow was precisely controlled with a continuous flow rate of 10 mL∙min-1 via a mass flow controller (MC-200SCCM-D/5M, Alicat Scientific, Inc.). The presented current density was normalized to the geometric surface area. All experiments were carried out at room temperature. The potentials for eNRR were corrected using the automatic iR-compensation function on the potentiostat.

For a standard experiment, all chambers were in working conditions for 30 mins to reach steady state. 2 mL of the catholyte was taken to determine the initial NH3 concentration as baseline. Subsequently, 2 hours chronoamperometry measurement was conducted with a constant applied potential vs. RHE. Afterward, 2 mL of the catholyte was taken to determine the final NH3 concentration. The eNRR synthesized NH3 was calculated based on the difference of the final and initial NH3 concentrations. The concentration of NH3 and N2H4 were detected by the Berthelot reaction using indophenol blue method, Nessler’s reagent method, and Watt and Chrisp’s method, which were described below.

For washing, a fresh 0.1 M KOH solution (100 mL) was then pumped for 30 min for 5 times, to remove any NH3 adsorbed on the inner surface of the reactor, vessels, and tubes. Finally, all components were disassembled and flushed with deionized water. In this work, the ion exchange membrane was cleaned after each experiment using the following procedure to remove any NH3 adsorbed on the membrane: (i) soak in the 1 mol/L KOH solution for 1 day, (ii) clean the membrane surface with fresh 1 mol/L KOH solution 3 times and repeat step (i) 3 times, (iii) clean the membrane surface with deionized water and leave the membrane in a gastight box filled with deionized water for the next usage.

Analysis of Ammonia by the Indophenol Blue Method

In a typical procedure, a tube vessel was used, and 2 mL of either a standard ammonia solution or a sample from the experiment was added to it. Subsequently, 2 mL of a 1 M sodium hydroxide aqueous solution containing 5 wt. % salicylic acid and 5 wt. % sodium citrate were introduced to the tube vessel. This was followed by the addition of 1 mL of 0.05 M sodium hypochlorite solution and 0.2 mL of 1 wt. % sodium nitroferricyanide aqueous solution. After allowing it to sit at room temperature for 2 hours, the absorption spectrum was measured using a UV-vis spectrophotometer. The presence of indophenol blue was determined by measuring the absorbance at a wavelength of 655 nm. To calibrate the concentration-absorbance curves, standard ammonium chloride solutions with various dilution factors (100, 50, 25, 10, 5, 1, 0.5 and 0 μM) were employed.

Analysis of Ammonia by the Nessler’s Reagent Method

In typical procedure, a tube vessel was used, and 2 mL of either a standard ammonia solution or a sample from the experiment was added to it. Subsequently, 2 mL of DI-water, 0.2 mL Nessler’s reagent (Hach cat.2119449) and 0.2 mL Rochelle salt (0.2 M KNaC4H4O6) were introduced to the tube vessel. After allowing it to sit at room temperature for 20 minutes, the absorption spectrum was measured using a UV-vis spectrophotometer. The presence of ammonia was determined by measuring the absorbance at a wavelength of 422 nm. To calibrate the concentration-absorbance curves, standard ammonium chloride solutions with various dilution factors (100, 50, 25, 10, 5, 1, 0.5 and 0 μM) were employed.

Determination of Hydrazine

The hydrazine (N2H4) production was determined by the method of Watt and Chrisp. In detail, a mixture of para(dimethylamino) benzaldehyde (5.99 g), HCl (concentrated, 30 mL) and ethanol (300 mL) were used as the color reagent. 2 mL of catholyte was mixed with 2 mL of color reagent and stay for 20 mins at room temperature, the UV-Vis absorption spectrum was obtained at a wavelength of 455 nm. The concentration-absorbance curves were calibrated using standard N2H4·H2O solutions with a series of concentrations in 0.1M KOH solution.

Analysis of Ammonia by Nuclear Magnetic Resonance (NMR) with 15N Labelling

The NRR experiments were performed using either 15N2 (99% isotopic purity, Sigma Aldrich) for isotopic labelling or normal 14N2 for comparison. Each NRR experiment was conducted at −0.20 V vs. RHE for 2 h. A 2 mL aliquot of the test solution was taken from the catholyte. A 500 μL aliquot of the resultant solution was added into an NMR tube, and 10 vol. % D2O was added for the lock signal and internal standard. The ammonia concentration was quantified by measuring the 1H NMR spectra for 14NH4+ or 15NH4+. The corresponding absolute calibration curves were obtained by using the 15NH4Cl (98.5% isotopic purity) and 14NH4Cl (dissolved in 0.1 M KOH) aqueous solutions with a series of known concentrations as the standards.

    - Calculations of NH3 Yield rate and Faradaic Efficiency (FE)

NH3 yield was calculated using the following equation:

Yield = [NH4+]×V/(m×t)	(3)

FE was calculated according to following equation:

FF = 3×F×[NH4+]×V/(17×Q)		(4)

In which, [NH4+] is the measured NH4+ concentration; V is the volume of the catholyte; t is the potential applied time; m is the loaded quantity of catalyst; F is the Faraday constant; and Q is the quantity of applied electricity.

Optimization of GDE

It is generally believed that a moderate thickness of catalyst layer (CL) and a uniform distribution of catalysts benefit achieving high eNRR performance. In our typical GDE fabrication process, a mixture of catalysts, Nafion, and PTFE in ethanol solution was sprayed on the carbon black side of the commercially purchased gas diffusion layer (GDL). The thickness of the catalyst layer was tuned by the catalyst loading from 0.5 to 2.5 mg∙cm-2. Afterward, the surface distribution was examined via SEM. As depicted in Figure S16, the commercial GDL was found to have large cracks. With an increase in the loading amount, the cracks gradually disappeared. When the loading reached 2.5 mg∙cm-2, no significant cracks were observed.  Meanwhile, the Faradaic efficiencies and NH3 yield rate kept increasing with the loading amount (Figure S17). However, the NH3 yield rate plateaued at a loading of 2.0 mg∙cm-2, indicating an optimal catalyst loading. Recent studies suggest that cracks are beneficial for mitigating flooding in GDE and preventing flooding-related performance drops, which may explain the observed performance trends. Another paramount property of GDE is surface wettability. The Mo/C-N GDE with varying surface wettability was tuned by adjusting the amount of hydrophobic agent PTFE (From 0 to 10 wt. %) while maintaining optimal catalyst loading in the spraying suspension. The measured contact angle increased with the PTFE content, as shown in Figure S18, indicating enhanced hydrophobicity. Consequently, as shown in Figure S19, the Faradaic efficiency was observed to decrease, while the NH3 yield rate increased. This suggests the increase in the hydrogen evolution reaction (HER) competed with the eNRR process. Therefore, a trade off point with a PTFE content of 7.5 wt. % was chosen.

Machine Learning

Two extreme gradient boosting (XGBoost) regression models were fitted to the complete dataset of 23 experimental records (Table S3), one for each target. The four inputs were average pore size, PTFE amount, catalyst loading, and Mo content. The targets were Faradaic efficiency and NH₃ yield. Both models used 300 trees, a learning rate of 0.05, a maximum tree depth of 6, a subsample ratio of 0.8, a column subsample ratio of 0.8, and a random seed of 42. These settings were specified directly in the analysis code. No hyperparameter optimization was performed.

Each model was fitted to all 23 records. We did not use a train/test split, k fold cross validation, repeated cross validation, or an independent test set. Folds and repeats are therefore not applicable. R², root mean square error (RMSE), and mean absolute error (MAE) were calculated from the same training data (Figure S24 and Table S4). These values measure the fit to the training data rather than performance on new data. SHAP values were also calculated from the complete dataset. They describe feature contributions only within the sampled ranges. Analyses were conducted in Python using the xgboost, scikit-learn, and shap packages.

RESULTS AND DISCUSSION

Structural features and elemental composition of the Mo porous carbon catalyst

Our synthesis of Mo-N/C (Figure 1) began with amphiphilic PS-b-PEO BBCP templates, dopamine as a carbon source, and a molybdenum precursor in a water/ethanol mixture, following our previously reported procedure.16 20 The mixture underwent rapid photothermal pyrolysis21 using a xenon flash lamp (Figure S1) with varying irradiation energies. At 2.61 J·cm-2 per pulse, the BBCP templates were fully removed, and a porous carbon structure was formed within 5 s. During synthesis and pyrolysis, Mo ions coordinate with nitrogen and oxygen to form Mo-Nx sites, while neighboring Mo atoms generate Mo-Mo nanoparticles encapsulated by a graphitized carbon shell, stabilizing them within the Mo-N/C framework. The short, rapid process preserved the spherical pore morphology as shown in Figure 2b and limited uncontrolled particle growth.

The optimized Mo-N/C catalyst, with a total metal loading of 4 wt% (determined through systematic loading optimization, discussed later), was comprehensively characterized using high-angle annular dark-field scanning transmission electron microscopy (HAADF-STEM). The HAADF-STEM images (Figures 2a and 2b) revealed the coexistence of ultrasmall Mo metal nanoparticles with an average diameter of approximately 1 nm and a high density of atomically dispersed Mo single atoms. These isolated Mo atoms were spatially separated from both clusters and nanoparticles and expected to act as conventional single-atom active sites. High-resolution

Figure 1.  Schematic representation of the synthesis process for preparing Mo-N/C ordered porous materials using photothermal pyrolysis.

transmission electron microscopy (HRTEM) further confirmed the presence of a limited population of Mo nanoparticles encapsulated within the carbon framework. Both the nanoparticles and the atomically dispersed Mo species were uniformly distributed throughout the porous carbon matrix, providing many accessible active sites. Elemental mapping (Figure S2) demonstrated a homogeneous distribution of Mo, N, O, and C across the entire sample, indicating successful incorporation of Mo species into the nitrogen-doped carbon support.

The pore structure of the Mo-N/C catalyst is tailored with the spherical micelle template by adjusting the micelle diameter. Specifically, the micelle diameter is precisely regulated by adjusting the molecular weight of the BBCP, where higher molecular weight leads to larger micelles (Figure S3). Five spherical micelles with diameters of 8, 30, 50, 75, and 100 nm were used as templates. Following photothermal pyrolysis, statistical pore-size analysis combined with TEM characterization (Figures S4 and S5) revealed well-defined pore diameters of 8, 15, 21, 33, and 56 nm. Accordingly, the samples are denoted as Mo/C-N-8, Mo/C-N-15, Mo/C-N-21, Mo/C-N-33, and Mo/C-N-56. Brunauer-Emmett-Teller (BET) surface area measurements (Figure S6) confirmed that all samples exhibited high specific surface areas, arising from a micro- and mesoporous architecture. This porous structure is expected to facilitate efficient mass transport and maximize the exposure of active Mo sites. X-ray diffraction (XRD) patterns (Figure S7) showed no distinct diffraction peaks associated with crystalline Mo phases,22, 23 suggesting that the Mo species were predominantly amorphous or atomically dispersed within the carbon matrix, consistent with the microscopy observations. These microscopic and structural characterizations demonstrate the successful synthesis of a porous Mo-N/C catalyst featuring uniformly distributed Mo single atoms and ultrasmall nanoparticles, a combination that is well suited for high catalytic activity due to the synergistic availability of isolated atomic sites and sub-nanometer metal domains.

Figure 2. Morphological and composition characterization of the sample. (a) STEM-HAADF image showing isolated Mo atoms and Mo clusters in graphitic lattice planes, with some Mo single atoms indicated by green circles. The scale bar is 2 nm. (b) HRTEM image reveals the typical ordered porous structure. The scale bar is 200 nm. (Insert: HRTEM image illustrating both ordered and disordered graphitic structures (turbostratic carbon) with Mo nanoparticles embedded within the graphitic matrix. The scale bar is 5 nm.) (c) Mo K-edge XANES of 4 and 1 wt. % Mo/C-N, Mo metal powder, MoO2, MoO3 and Mo2C. (d) Fitting of FT EXAFS spectra of 4 wt. % Mo/C-N.

To probe the local coordination structure and electronic state of Mo in the Mo-N/C catalyst with a total metal loading of 4 wt%, Mo K-edge X-ray absorption spectroscopy (XAS) was performed using Mo foil (Mo0), MoO2 (Mo4+), and MoO3 (Mo6+) as reference materials. A Mo-N/C sample with a lower metal loading (1 wt%) was also examined to evaluate how variations in Mo loading affect the local atomic environment and catalytic behavior, as discussed in the electrochemical section. As shown in Figure 2d, XANES spectra of both 4 and 1 wt% Mo-N/C exhibit edge positions close to that of metallic Mo foil and slightly shifted to higher energy, while remaining at significantly lower energies than those of MoO2 and MoO3. The edge position was also marginally lower than that of Mo2C (Mo4+), indicating that Mo in Mo-N/C existed in a reduced electronic state.24 These features indicated a mixed-valence configuration between Mo0 and Mo4+, with Mo4+ as the major oxidation state. This assignment was consistent with XPS analysis (Figures S8a and S8c), which reveals Mo 3d binding energies corresponding to Mo0 (228.1 eV, 45%) and Mo4+ (232.4 eV, 55%).25 Fourier-transformed extended X-ray absorption fine structure (FT-EXAFS) analysis provided further insight into the local atomic structure. As shown in Figure S9, Mo-N/C exhibited a pronounced peak at 2.60 Å, attributed to Mo-Mo coordination, confirming the presence of ultrasmall Mo nanoparticles. Additional peaks at 1.46 Å and 1.11 Å corresponded to Mo-C and Mo-N coordination, respectively, indicating the coexistence of atomically dispersed Mo species anchored within the nitrogen-doped carbon matrix.26, 27 Quantitative fitting of the EXAFS R-space spectra (Figures 2d and S10) yielded low R-factors of 0.011 and 0.025 for the 4 and 1 wt% Mo-N/C samples, respectively, demonstrating excellent agreement between the experimental data and the proposed structural model (Table S1). XPS analysis (Figure S11) further elucidated the carbon framework in Mo-N/C. The C 1s spectrum shows peaks at 284.3, 286.1, and 287.3 eV, corresponding to sp2 C-C, C-N, and C=O species, respectively, indicating a heteroatom-doped carbon matrix with mixed ordered and disordered graphitic domains.28 This was supported by the high-resolution O 1s spectrum, which displayed components at 532.2 and 533.4 eV, attributed to hydroxyl groups and carbon-oxygen functionalities, respectively (Figure S8d).29 A minor sp3 C-C contribution at 284.7 eV suggested incomplete graphitization and the presence of structural defects within the carbon matrix. Thus, the spectroscopic analyses lead to four key conclusions: (i) Mo existed predominantly in a mixed-valence state, with Mo4+ as the major oxidation state, with a substantial fraction of reduced Mo0 species; (ii) the catalyst contained both atomically dispersed Mo/C-N sites and highly disordered Mo-Mo ultrasmall nanoparticles; (iii) the defect-rich, nitrogen-doped carbon matrix played a critical role in stabilizing these Mo species, enabling the formation of an atomic-scale heterostructure favorable for catalytic applications; and (iv) increasing the metal loading from 1 to 4 wt% did not significantly alter the local coordination environment, oxidation state of Mo, or bonding with heteroatoms. This indicated that, up to 4 wt%, the local structure remained essentially unchanged, and any differences in catalytic performance are likely attributable.

Electrochemical performance evaluation for ammonia synthesis via nitrogen reduction

Since ammonia production in eNRR is strongly influenced by catalyst structure and electrode architecture, we systematically investigated how Mo content and applied potential affect the performance under room temperature and atmospheric pressure. The as-synthesized Mo/C-N catalysts were first screened in H-type cells using 0.1 M HCl, 0.1 M Na2SO4, and 0.1 M KOH electrolytes, showing activity only in KOH, which was therefore employed for subsequent experiments (Figure S12). Catalysts were then deposited on a GDE and integrated into a flow cell comprising the anolyte, catholyte, and gas supply compartments separated by an anion exchange membrane to prevent NH3 crossover (Figures S13 and 3a). Mo/C-N GDE and 40 wt.% Pt/C on carbon cloth served as the cathode and the anode, respectively, with an Ag/AgCl reference electrode forming a three-electrode system. N2 was supplied (Figure S14) at 10 mL∙min⁻¹ and purified to remove NOx, while the 30 mL catholyte and anolyte were circulated with controlled flow, maintaining stable electrolyte pressure.30 N2 diffused through the porous GDE, generating a gas-solid-liquid three-phase interface on the catalyst surface (Figure 3b) that facilitated eNRR through proton and electron transfer at the active sites.

To evaluate the effect of Mo content, catalysts with varying loadings were prepared and tested. Both Faradaic efficiency and NH3 yield increased with (Figure 3c) Mo content up to 4 wt.% but declined at higher loadings, attributed to aggregation and the formation of larger particles, which reduce electrochemically accessible active sites. Electrochemically active surface area (ECSA) measurements confirmed this trend, with maximum ECSA observed at 4 wt.% Mo (Figures 3d and 3e). This loading was therefore selected as optimal, balancing high active-site density with minimal aggregation and reduced activation polarization. Subsequently, the applied potential was optimized (Figure 3f), with -0.2 V vs. RHE yielding the highest Faradaic efficiency and NH3 production.

Figure 3. Gas-diffusion flow cell architecture and nitrogen reduction performance. (a) Schematic illustration of gas diffusion flow cell, (b) gas-solid-liquid three-phase interface on the gas diffusion electrode. (c) Faradaic efficiencies and NH3 yield rate of Mo-N/C catalysts in different Mo contents (wt. %) in optimized conditions. (d) Plots of capacitive current density vs. scan rate for as-synthesized Mo/N-C catalysts in different Mo contents (wt. %) in a non-Faradaic range (0.1-0.3 V vs. RHE). (e) Plots of calculated double-layer capacitance (Cdl) values vs. Mo contents. f) Faradaic efficiencies and NH3 yield rate of 4 wt. % Mo/C-N-21 GDE applied at -0.1, -0.2, -0.3, -0.4, and -0.5 V vs. RHE in flow cell.

FTIR spectroscopy revealed (Figures S15) the progressive growth of peaks corresponding to H-N-H bending, -NH2 wagging, and N-N stretching of adsorbed N2Hy (1<y<4), consistent with an associative N2-to-NH3 reaction pathway reported for Mo-based catalysts.31, 32 To confirm the origin of NH3 and exclude false positives, control experiments were conducted with Ar, a blank GDE, and no applied potential, all showing negligible NH3 formation (Figures S16 and S17). Isotope-labeling with 15N2 further verified that the detected NH3 originated from the supplied nitrogen. Two peaks representing 15NH3 were identified in the sample after the reaction, which is consistent with the control experiments.33, 34 The increased detection of NH3 can be attributed to the electrocatalytic reduction of the supplied N2 in the experiment (Figures S18). The efficiency of a GDE flow cell is largely determined by the quality of the GDE, including factors such as thickness, surface morphology, and properties, which are influenced by the fabrication process and composition.35, 36 Hence, GDE properties including catalyst loading, PTFE content, and membrane quality were optimized (Figures S19 to S22), identifying 2.0 mg cm-2 catalyst loading with 7.5 wt.% PTFE was ideal for stable electrolyte flow, effective three-phase interface formation, and reproducible eNRR performance. Based on these results, the optimized 4 wt.% Mo/C-N catalyst achieved 34.7 µg h-1 mg-1 of NH3 production with 21.6 % of Faradaic efficiency, which indicated that precise control of active-site density and electrode architecture was critical for high-performance eNRR in flow-cell systems.

Influence of pore structure and catalyst parameters on eNRR performance

In gas-diffuse reactions, pores serve as mass transport channels, facilitating access to both the electrolyte and N2 reactant. These channels play a critical role in forming the gas-solid-liquid three-phase interface. As shown in Figure 4a, Faradaic efficiency and NH3 yield decreased sharply when the actual pore size exceeded 21 nm. Meanwhile, the ECSA increased from 8 nm to 21 nm (Figures 4b and 4c) but declined for larger pore sizes, likely because micropores and macropores contribute less to accessible active sites. To analyze the electrochemical behavior of the GDE, two equivalent circuits were established based on the proposed three-phase interface (Figure 4d). Nyquist plots of the optimized 4 wt.% Mo/C-N-21 GDE under N₂ and Ar feeding are shown in Figure 4e. The solution resistance (Rs), representing electrolyte resistance, and Rct/Rp, corresponding to the charge transfer resistance of the anion exchange membrane (AEM), remained unchanged, consistent with their non-Faradaic behavior. In contrast, introducing N2 generated an additional semicircle in the high-frequency region, indicating a Faradaic charge transfer resistance associated with eNRR. Variation of Rct with applied potential (Figure S23) confirmed its Faradaic nature. After systematically altering pore sizes while keeping other parameters constant, Nyquist plots and calculated resistances (Figure 4f and Table S2) revealed that Rct increased with larger pore sizes. This indicates that micropores retain N2 near the catalyst surface, promoting eNRR while suppressing the competing hydrogen evolution reaction.37 These results demonstrated that pore structure influenced both activation and diffusion polarization, though distinguishing the dominant factor requires further analysis.

Figure 4. Pore-size dependent nitrogen reduction performance and interfacial charge-transfer behavior. (a) Faradaic efficiencies and NH3 yield rate of 4 wt. % Mo/N-C catalysts with different average pore sizes in optimized conditions. (b) Plots of capacitive current density vs. scan rate for 4 wt. % Mo/N-C catalysts with different average pore sizes in a non-Faradaic range (0.1-0.3 V vs. RHE). (c) Plots of calculated double-layer capacitance (Cdl) values vs. average pore size. (d) Schematic of gas-solid-liquid three-phase interface on catalysts’ surface and proposed equivalent circuits. (e) Nyquist plots of 4 wt. % Mo-N/C-21 recorded in Ar and N2 conditions. (f) Nyquist plots of 4 wt. % Mo/N-C with different average pore sizes recorded in N2 conditions

Machine learning analysis of performance-determining factors

After assessing the effects of pore size, Mo content, catalyst loading, and wettability on eNRR performance, we used XGBoost and SHAP to explore the 23 available experimental records. The two fitted models relate the four controlled input variables to Faradaic efficiency and NH₃ yield, respectively (Figure S24). The dataset consists mainly of experimental series in which one variable was changed at a time. It is not a balanced multivariable design. We therefore use the analysis to summarize associations within the investigated ranges. When evaluated using the observations used for fitting, the Faradaic efficiency model gave R² = 1.000, RMSE ≈ 0.090 percentage points, and MAE = 0.069 percentage points. The NH₃ yield model gave R² = 1.000, RMSE ≈ 0.235 µg h⁻¹ mg⁻¹, and MAE = 0.180 µg h⁻¹ mg⁻¹ (Table S4). These values measure fit to the same data used to build the models. They do not independently test how well the models generalize. SHAP values describe how each feature contributes to the fitted prediction relative to the model baseline. They do not establish causal or mechanistic effects.

Figure 5. Machine learning analysis of NRR performance. SHAP analysis and feature importance ranking for the XGBoost models fitted to (a) Faradaic efficiency and (b) NH₃ yield. A larger absolute SHAP value indicates a larger contribution of that feature to the fitted prediction. The sign indicates whether the predicted target increases or decreases relative to the model baseline. Dot color represents the numerical feature value, from low (blue) to high (red). The plots summarize associations within this dataset and the sampled ranges. They should not be interpreted as causal effects or universal feature rankings.

Within this dataset, Mo content showed the largest overall SHAP magnitudes for both targets. For Faradaic efficiency, the fitted ranking was Mo content, catalyst loading, PTFE amount, and average pore size. For NH₃ yield, the fitted ranking was Mo content, average pore size, PTFE amount, and catalyst loading. The distributions also suggest nonmonotonic behavior, with favorable fitted contributions near the middle of the sampled Mo range. These observations show that Mo content is an important variable in the present experiments. They do not prove that it always dominates activation polarization or that pore structure is generally secondary. The analysis is limited by a sample size of 23, only four controlled variables, experimental series in which one variable was changed at a time, and the absence of independent or external validation. The feature rankings may depend on the ranges and density with which the variables were sampled. A larger multivariable dataset collected with independent sampling will be needed to test the robustness and broader applicability of these trends.

Stability and two-electrode cell performance

Beyond activity, stability is a critical metric for evaluating electrocatalysts. The optimized 4 wt.% Mo-N/C-21 GDE was subjected to five repetitive 2-hour eNRR cycles and a continuous 10-hour test at -0.2 V vs. RHE (Figure S25). The cathodic current remained stable around 0.8 mA cm⁻², and NH3 yield stabilized at ~34 µg h-1 mg-1, demonstrating excellent operational stability. Morphological analysis before and after 10 hours of electrolysis (Figure S26) revealed no significant changes in surface structure or pore architecture, indicating that the carbon substrate provides robust structural support. XPS analysis (Figure S27) showed an increase in the metallic Mo fraction from 45 % to 62%, corresponding to partial reduction of Mo4+ to Mo0, which ensures sustained catalytic activity. The combination of stable morphology and consistent composition under long-term operation confirms the durability of the Mo/C-N catalyst. Its performance was comparable to or exceeds that of most previously reported eNRR electrocatalysts (Figure S28 and Table S5). The practical performance of the GDE flow cell was further evaluated using a two-electrode system under DC voltage. As shown in Figure S29a, current density plateaued at ~2.6 V, indicating diffusion-limited N2 transport. Faradaic efficiency reached a maximum at 1.9 V before declining, likely due to increasing HER. V-I curves (Figure S29b) demonstrated that power density increased with applied voltage, reaching a maximum of 0.21 W cm⁻² at 1.9 V, highlighting the cell’s capability for efficient ammonia production under practical operating conditions.

CONCLUSIONS

In conclusion, we developed Mo single-atom and nanoparticle catalysts anchored on mesoporous nitrogen-doped carbon via ultra-fast photothermal pyrolysis of BBCP templates, establishing that 4 wt.% Mo provided the highest electrochemically accessible active-site density while 21 nm pores maximized the gas-solid-liquid interface, retained N2 at active sites, and suppressed HER. The optimized 4 wt.% Mo/C-N catalyst achieved a Faradaic efficiency of 21.6 % and an NH3 yield of 34.7 μg h⁻¹ mg⁻¹ at -0.2 V vs. RHE in 0.1 M KOH, maintaining stable activity over five 2-hour cycles and a 10-hour continuous operation. Spectroscopic analyses revealed that metallic Mo acted as the primary active site, with time-dependent growth of H-N-H bending, -NH2 wagging, and N-N stretching peaks of adsorbed N2Hy species confirming an associative N2-to-NH3 pathway, while XPS showed the Mo retained its reduced state during prolonged electrolysis. Optimizing the GDE with 2.0 mg cm-2 catalyst loading and 7.5 wt.% PTFE ensured stable electrolyte flow, effective triple-phase interface formation, and reproducible eNRR activity. Exploratory XGBoost and SHAP analysis of the 23 records found that Mo content had the largest fitted contribution for both targets. Catalyst loading, wettability, and pore size showed different contributions for the two targets within the investigated ranges. The analysis included only four variables from a small dataset. The experiments also followed a one variable at a time sampling structure and lacked independent validation. The results should therefore be viewed as trends within this dataset. They are not universal design principles. The experimental results clarify how structural, compositional, and interfacial parameters affect this catalyst and flow cell system. The machine learning analysis provides hypotheses that can be tested using larger datasets with independent sampling.

ACKNOWLEDGMENTS

The authors would like to acknowledge the Penn State Materials Characterization Lab providing access to the XPS instrument, and the facility services for electron microscopy and spectroscopy at the Department of Polymer Science and Engineering, as well as the Institute of Applied Sciences at the University of Massachusetts, Amherst, USA. Special thanks are extended to the Watkins group members, particularly Dr. Takumi Uchiyama, Karan Sagar, and Varun Pande, as well as the Wu group members, for their fruitful discussions. Part of the electron microscopy was conducted at CCEM-McMaster University (with support from Dr. Carmen Andrei), a national facility supported by NSERC Canada. The authors also thank the National Synchrotron Radiation Research Center (Taiwan) for beamtime allocation for XAS measurements. Financial support from the US Army Research Laboratory (under the National Center for Manufacturing Sciences, award number HQ0034-15-2-0007, and Expeditionary Maneuver Support award number W911QY1990011), as well as the Office of Naval Research (under LIFT award number N000142190010) are greatly acknowledged. The authors used ChatGPT solely for language polishing and did not use it to write the original manuscript or generate any data.

AUTHOR CONTRIBUTIONS

Chaoyung Tang, and Dipankar Saha equally contributed to this work. Chaoyung Tang, Dipankar Saha, Nianqiang Wu, and James J. Watkins conceived the project and designed the experiments. Chaoyung Tang and Dipankar Saha carried out the experiments and performed data analysis with input from Nianqiang Wu and James J. Watkins. Connor L. Witt contributed to bottlebrush polymer synthesis. Wei Fan conducted a BET measurement. Arvind Chandrasekar and Chung-Li Dong conducted XANES and EXAFS measurements. Yulei Wang and Zhu Chen for the electrochemistry discussion. Negar Sabouhanian and Aicheng Chen carried out IR measurements. Jiacheng Wang performed the theoretical calculations. All authors contributed to data interpretation and discussion. The manuscript was written by Dipankar Saha and Chaoyung Tang, with the theoretical section written by Jiacheng Wang, and was revised with input from all co-authors.

COMPETING INTERESTS

Chaoyun Tang, Dipankar Saha, James J. Watkins, and Nianqiang Wu have filed for a provisional U.S. patent covering the synthesis process and application described in this manuscript.

REFERENCES

(1) Qing, G.; Ghazfar, R.; Jackowski, S. T.; Habibzadeh, F.; Ashtiani, M. M.; Chen, C.-P.; Smith, M. R., III; Hamann, T. W. Recent Advances and Challenges of Electrocatalytic N2 Reduction to Ammonia. Chemical Reviews 2020, 120 (12), 5437-5516. DOI: 10.1021/acs.chemrev.9b00659.

(2) Zhao, X.; Hu, G.; Chen, G.-F.; Zhang, H.; Zhang, S.; Wang, H. Comprehensive Understanding of the Thriving Ambient Electrochemical Nitrogen Reduction Reaction. Advanced Materials 2021, 33 (33), 2007650. DOI: https://doi.org/10.1002/adma.202007650.

(3) Shi, L.; Yin, Y.; Wang, S.; Sun, H. Rational Catalyst Design for N2 Reduction under Ambient Conditions: Strategies toward Enhanced Conversion Efficiency. ACS Catalysis 2020, 10 (12), 6870-6899. DOI: 10.1021/acscatal.0c01081.

(4) Wang, S.; Ichihara, F.; Pang, H.; Chen, H.; Ye, J. Nitrogen Fixation Reaction Derived from Nanostructured Catalytic Materials. Advanced Functional Materials 2018, 28 (50), 1803309. DOI: https://doi.org/10.1002/adfm.201803309.

(5) Kolen, M.; Ripepi, D.; Smith, W. A.; Burdyny, T.; Mulder, F. M. Overcoming Nitrogen Reduction to Ammonia Detection Challenges: The Case for Leapfrogging to Gas Diffusion Electrode Platforms. ACS Catalysis 2022, 12 (10), 5726-5735. DOI: 10.1021/acscatal.2c00888.

(6) Zou, H.; Rong, W.; Wei, S.; Ji, Y.; Duan, L. Regulating kinetics and thermodynamics of electrochemical nitrogen reduction with metal single-atom catalysts in a pressurized electrolyser. Proceedings of the National Academy of Sciences 2020, 117 (47), 29462-29468. DOI: doi:10.1073/pnas.2015108117.

(7) Jiang, L.; Bai, X.; Zhi, X.; Jiao, Y. New Mechanistic Insights into Electrokinetic Competition Between Nitrogen Reduction and Hydrogen Evolution Reactions. Advanced Energy Materials 2024, 14 (28), 2303809. DOI: https://doi.org/10.1002/aenm.202303809.

(8) Sengupta, K.; Joyce, J. P.; Decamps, L.; Kang, L.; Bjornsson, R.; Rüdiger, O.; DeBeer, S. Investigating the Molybdenum Nitrogenase Mechanistic Cycle Using Spectroelectrochemistry. Journal of the American Chemical Society 2025, 147 (2), 2099-2114. DOI: 10.1021/jacs.4c16047.

(9) Raju, R. K. Electrocatalytic reduction of nitrogen to ammonia on metal nanoclusters: insights and trends from d- and p-block metals. Physical Chemistry Chemical Physics 2025, 27 (15), 7773-7796, 10.1039/D5CP00046G. DOI: 10.1039/D5CP00046G.

(10) Mao, X.; Bai, X.; Wu, G.; Qin, Q.; O’Mullane, A. P.; Jiao, Y.; Du, A. Electrochemical Reduction of N2 to Ammonia Promoted by Hydrated Cation Ions: Mechanistic Insights from a Combined Computational and Experimental Study. Journal of the American Chemical Society 2024, 146 (27), 18743-18752. DOI: 10.1021/jacs.4c06629.

(11) Chen, J.; Wang, H.; Wang, Z.; Mao, S.; Yu, J.; Wang, Y.; Wang, Y. Redispersion of Mo-Based Catalysts and the Rational Design of Super Small-Sized Metallic Mo Species. ACS Catalysis 2019, 9 (6), 5302-5307. DOI: 10.1021/acscatal.8b04634.

(12) Guo, X.; Wan, X.; Shui, J. Molybdenum-based materials for electrocatalytic nitrogen reduction reaction. Cell Reports Physical Science 2021, 2 (6). DOI: 10.1016/j.xcrp.2021.100447 (acccessed 2026/01/22).

(13) Suryanto, B. H. R.; Du, H.-L.; Wang, D.; Chen, J.; Simonov, A. N.; MacFarlane, D. R. Challenges and prospects in the catalysis of electroreduction of nitrogen to ammonia. Nature Catalysis 2019, 2 (4), 290-296. DOI: 10.1038/s41929-019-0252-4.

(14) Monteiro, M. C. O.; Philips, M. F.; Schouten, K. J. P.; Koper, M. T. M. Efficiency and selectivity of CO2 reduction to CO on gold gas diffusion electrodes in acidic media. Nature Communications 2021, 12 (1), 4943. DOI: 10.1038/s41467-021-24936-6.

(15) Sun, Z.; Ma, T.; Tao, H.; Fan, Q.; Han, B. Fundamentals and Challenges of Electrochemical CO2 Reduction Using Two-Dimensional Materials. Chem 2017, 3 (4), 560-587. DOI: https://doi.org/10.1016/j.chempr.2017.09.009.

(16) Saha, D.; Tang, C.; Khan, J.; Jain, P.; Yang, C.-J.; Dong, C.-L.; Webster, R. F.; Chen, C.-L.; Chen, Z.; Bai, P.; et al. Alkaline electrocatalytic water oxidation by Fe–Ni nanostructures on porous turbostratic carbon with tailorable metal–metal active sites. Chemical Science 2026, 10.1039/D5SC05330G. DOI: 10.1039/D5SC05330G.

(17) Saha, D.; Yu, H.-J.; Wang, J.; Prateek; Chen, X.; Tang, C.; Senger, C.; Pagaduan, J. N.; Katsumata, R.; Carter, K. R.; et al. Mesoporous Single Atom-Cluster Fe–N/C Oxygen Evolution Electrocatalysts Synthesized with Bottlebrush Block Copolymer-Templated Rapid Thermal Annealing. ACS Applied Materials & Interfaces 2024, 16 (11), 13729-13744. DOI: 10.1021/acsami.3c18693.

(18) Saha, D.; Witt, C. L.; Fatima, R.; Uchiyama, T.; Pande, V.; Song, D.-P.; Fei, H.-F.; Yavitt, B. M.; Watkins, J. J. Opportunities in Bottlebrush Block Copolymers for Advanced Materials. ACS Nano 2025, 19 (2), 1884-1910. DOI: 10.1021/acsnano.4c12021.

(19) Saha, D.; Bhardwaj, A.; Wang, J.; Pande, V.; Hengstebeck, R.; Bai, P.; Watkins, J. J. Probing Electrocatalytic Synergy in Graphene/MoS2/Nickel Networks for Water Splitting through a Combined Experimental and Theoretical Lens. ACS Applied Materials & Interfaces 2024, 16 (32), 42254-42269. DOI: 10.1021/acsami.4c08869.

(20) Fei, H.-F.; Long, Y.; Yu, H.-J.; Yavitt, B. M.; Fan, W.; Ribbe, A.; Watkins, J. J. Bimodal Mesoporous Carbon Spheres with Small and Ultra-Large Pores Fabricated Using Amphiphilic Brush Block Copolymer Micelle Templates. ACS Applied Materials & Interfaces 2020, 12 (51), 57322-57329. DOI: 10.1021/acsami.0c16566.

(21) Song, D.-P.; Li, W.; Park, J.; Fei, H.-F.; Naik, A. R.; Li, S.; Zhou, Y.; Gai, Y.; Watkins, J. J. Millisecond photothermal carbonization for in-situ fabrication of mesoporous graphitic carbon nanocomposite electrode films. Carbon 2021, 174, 439-444. DOI: https://doi.org/10.1016/j.carbon.2020.12.036.

(22) Fang, T.; Wang, J.; Bai, Z.; Wang, Y.; Wang, N.; Xiang, D.; Cai, K. Hydrogen Migration Mechanism: Hydrogen Spillover Effect Enables Enhanced Hydrogen Evolution Reaction on MoC@MoN Heterostructure in a Wide pH Range. ACS Applied Materials & Interfaces 2025, 17 (37), 52102-52111. DOI: 10.1021/acsami.5c11431.

(23) Saha, D.; Selvaganapathy, P. R.; Kruse, P. Peroxide-Induced Tuning of the Conductivity of Nanometer-Thick MoS2 Films for Solid-State Sensors. ACS Applied Nano Materials 2020, 3 (11), 10864-10877. DOI: 10.1021/acsanm.0c02135.

(24) Svyazhin, A.; Nalbandyan, V.; Rovezzi, M.; Chumakova, A.; Detlefs, B.; Guda, A. A.; Santambrogio, A.; Manceau, A.; Glatzel, P. Chemical Information in the L3 X-ray Absorption Spectra of Molybdenum Compounds by High-Energy-Resolution Detection and Density Functional Theory. Inorganic Chemistry 2022, 61 (2), 869-881. DOI: 10.1021/acs.inorgchem.1c02600.

(25) Lv, X.-W.; Liu, X.-L.; Suo, Y.-J.; Liu, Y.-P.; Yuan, Z.-Y. Identifying the Dominant Role of Pyridinic-N–Mo Bonding in Synergistic Electrocatalysis for Ambient Nitrogen Reduction. ACS Nano 2021, 15 (7), 12109-12118. DOI: 10.1021/acsnano.1c03465.

(26) Wharton, J. A.; Ross, D. H.; Treacy, G. M.; Wilcox, G. D.; Baldwin, K. R. An EXAFS investigation of molybdate-based conversion coatings. Journal of Applied Electrochemistry 2003, 33 (7), 553-561. DOI: 10.1023/A:1024911119051.

(27) Savinelli, R. O.; Scott, S. L. Wavelet transform EXAFS analysis of mono- and dimolybdate model compounds and a Mo/HZSM-5 dehydroaromatization catalyst. Physical Chemistry Chemical Physics 2010, 12 (21), 5660-5667, 10.1039/B926474D. DOI: 10.1039/B926474D.

(28) Fujimoto, A.; Yamada, Y.; Koinuma, M.; Sato, S. Origins of sp3C peaks in C1s X-ray Photoelectron Spectra of Carbon Materials. Analytical Chemistry 2016, 88 (12), 6110-6114. DOI: 10.1021/acs.analchem.6b01327.

(29) Zhang, Q.; Li, X.; Ma, Q.; Zhang, Q.; Bai, H.; Yi, W.; Liu, J.; Han, J.; Xi, G. A metallic molybdenum dioxide with high stability for surface enhanced Raman spectroscopy. Nature Communications 2017, 8 (1), 14903. DOI: 10.1038/ncomms14903.

(30) Choi, J.; Suryanto, B. H. R.; Wang, D.; Du, H.-L.; Hodgetts, R. Y.; Ferrero Vallana, F. M.; MacFarlane, D. R.; Simonov, A. N. Identification and elimination of false positives in electrochemical nitrogen reduction studies. Nature Communications 2020, 11 (1), 5546. DOI: 10.1038/s41467-020-19130-z.

(31) Yao, Y.; Zhu, S.; Wang, H.; Li, H.; Shao, M. A Spectroscopic Study on the Nitrogen Electrochemical Reduction Reaction on Gold and Platinum Surfaces. Journal of the American Chemical Society 2018, 140 (4), 1496-1501. DOI: 10.1021/jacs.7b12101.

(32) Li, P.; Zhou, Z.; Wang, Q.; Guo, M.; Chen, S.; Low, J.; Long, R.; Liu, W.; Ding, P.; Wu, Y.; Xiong, Y. Visible-Light-Driven Nitrogen Fixation Catalyzed by Bi5O7Br Nanostructures: Enhanced Performance by Oxygen Vacancies. Journal of the American Chemical Society 2020, 142 (28), 12430-12439. DOI: 10.1021/jacs.0c05097.

(33) Wilder, L. M.; Balogun, K.; Klein, W. E.; Chumble, P.; Young, J. L. Nitrogen Reduction Testing with Real-Time 15NH3 Yield Quantification Using Orbital Multiturn Time-of-Flight Mass Spectrometry. ACS Energy Letters 2024, 9 (12), 5780-5786. DOI: 10.1021/acsenergylett.4c02961.

(34) Wang, X.; Peng, X.; Chen, W.; Liu, G.; Zheng, A.; Zheng, L.; Ni, J.; Au, C.-t.; Jiang, L. Insight into dynamic and steady-state active sites for nitrogen activation to ammonia by cobalt-based catalyst. Nature Communications 2020, 11 (1), 653. DOI: 10.1038/s41467-020-14287-z.

(35) Kong, Y.; Liu, M.; Hu, H.; Hou, Y.; Vesztergom, S.; Gálvez-Vázquez, M. d. J.; Zelocualtecatl Montiel, I.; Kolivoška, V.; Broekmann, P. Cracks as Efficient Tools to Mitigate Flooding in Gas Diffusion Electrodes Used for the Electrochemical Reduction of Carbon Dioxide. Small Methods 2022, 6 (9), 2200369. DOI: https://doi.org/10.1002/smtd.202200369.

(36) Kong, Y.; Hu, H.; Liu, M.; Hou, Y.; Kolivoška, V.; Vesztergom, S.; Broekmann, P. Visualisation and quantification of flooding phenomena in gas diffusion electrodes used for electrochemical CO2 reduction: A combined EDX/ICP–MS approach. Journal of Catalysis 2022, 408, 1-8. DOI: https://doi.org/10.1016/j.jcat.2022.02.014.

(37) Saha, D.; Patel, V.; Selvaganapathy, P. R.; Kruse, P. Facile fabrication of conductive MoS2 thin films by sonication in hot water and evaluation of their electrocatalytic performance in the hydrogen evolution reaction. Nanoscale Advances 2022, 4 (1), 125-137, 10.1039/D1NA00456E. DOI: 10.1039/D1NA00456E.

(38) Chen, T.; Guestrin, C. XGBoost: A Scalable Tree Boosting System. In Proceedings of the 22nd ACM SIGKDD International Conference on Knowledge Discovery and Data Mining, San Francisco, California, USA; 2016.

(39) Lundberg, S. M.; Lee, S.-I. A unified approach to interpreting model predictions. In Proceedings of the 31st International Conference on Neural Information Processing Systems, Long Beach, California, USA; 2017.