Supporting Information

Chaoyun Tang,1+ Dipankar Saha,2+ Jiacheng Wang,1 Arvind Chandrasekar,3 Negar Sabouhanian,4 Connor L. Witt,2 Yulei Wang,1 Aicheng Chen,4 Wei Fan,1 Chung-Li Dong, 3 Zhu Chen,1 James J. Watkins,2* and Nianqiang Wu1*

1 Department of Chemical Engineering, University of Massachusetts, Amherst, MA 01002, United States

2Conte Center for Polymer Research, Department of Polymer Science and Engineering, University of Massachusetts, Amherst, MA 01002, United States

3Department of Physics, Tamkang University, New Taipei City, Taiwan

4Department of Chemistry, University of Guelph, Guelph, Canada

*Corresponding author’s email:

nianqiangwu@umass.edu and watkins@umass.edu

+ Equal Contribution

Figure S1. Scheme illustration of thermal pyrolysis instruments and processes.

Figure S2. HAADF-EDX elemental mapping indicates a homogeneous distribution of Mo, carbon, nitrogen, and oxygen atoms throughout the sample. The scale bar for all images is 2 nm.

Figure S3. Scheme illustration of brush polymer template adopted in experiments.

Figure S4. TEM images of as-synthesized samples derived from BBCP with estimated diameters of ) 8 nm, b) 15 nm, c) 21 nm, d) 33 nm, and e) 56 nm.

Figure S5. Statistics pore size distribution of as-synthesized samples derived from BBCP with estimated diameters of a) 8 nm, b) 15 nm, c) 21 nm, d) 33 nm, and e) 56 nm, respectively.

Figure S6. BET absorption/desorption curve of as-synthesized samples with pore size of a) 8 nm, b) 15 nm, c) 21 nm, d) 33 nm, and e) 56 nm.

Figure S7. XRD pattern of as-synthesized Mo/N-C material.

Figure S8. XPS spectra of Mo nanostructure: (a) Mo 3d, (b) O 1s, and (c) N 1s high-resolution spectra showing binding energy peaks for Mo, oxygen, and nitrogen species.

Figure S9. FT EXAFS spectra of 4 and 1 wt. % Mo/C-N, Mo metal powder, MoO2, MoO3 and Mo2C.

Figure S10. Fitting of FT EXAFS spectra of 1 wt. % Mo/C-N.

| Sample | Shell Position | N | σ2 (Å-2) | ∆E0 (eV) | R (Å) | R-Factor |
| --- | --- | --- | --- | --- | --- | --- |
| 4 wt. % Mo/C-N | Mo-N | 1.946 | 0.00211 | -7.766 | 1.74896 | 0.0107124 |
|  | Mo-C | 3.892 | 0.00872 | -7.766 | 1.99927 |  |
|  | Mo-Mo | 5.838 | 0.00991 | -7.766 | 2.97093 |  |
| 1 wt. % Mo/C-N | Mo-N | 1.542 | 0.00062 | -8.019 | 1.75026 | 0.0252494 |
|  | Mo-C | 3.084 | 0.00891 | -8.019 | 1.99616 |  |
|  | Mo-Mo | 4.626 | 0.00160 | -8.019 | 2.97196 |  |

Table S1. Fitting parameters of the Fourier-transformed EXAFS spectrum of Mo.

Figure S11. XPS spectra of as-synthesized 4 wt. % Mo/C-N-21 nanostructure: a) survey spectra and b) high resolution XPS spectra of C 1s.

Figure S12. Linear sweep voltammetry curves of typical 4 wt. % Mo/C-N-21 nanostructure catalyst record in H-type cells in different electrolyte: a) 0.1 M HCl, b) 0.1 M Na2SO4 and c) 0.1 M KOH.

Figure S13. Schematic illustration of the gastight electrochemical eNRR system.

Figure S14.  Using colorimetric method for detection and quantification of NH3 in 0.1 M KOH electrolyte after eNRR. a) The UV-Vis absorption spectrum of NH4+ with different concentrations using indophenol blue method, the characteristic peaks centered at 655 nm correspond to signals of NH4+. b) The standard curve showing the correlation of  NH4+ concentration with the absorbance peak centered at 655 nm. The error bars represent the standard deviation of over 3 times independent calibrations. c) The UV-Vis absorption spectrum of NH4+ with different concentrations using Nessler’s reagent method, the characteristic peaks centered at 422 nm correspond to signals of NH4+. d) The standard curve showing the correlation of  NH4+ concentration with the absorbance peak centered at 422 nm. The error bars represent the standard deviation of over 3 times independent calibrations.

Figure S15. Operando FTIR spectra of 4 wt. % Mo/C-N-21 under N2 purge at -0.2 V.

Figure S16. a) UV-Vis absorption spectra and b) corresponding calibration curve for the colorimetric N2H4 assay in 0.1 M KOH electrolyte.

Figure S17. A comparison of eNRR performance of Reference samples (4 wt. % Mo/C-N-21, loading: 2 mg∙cm-2) in different condition: (R) with a potential of -0.2 V vs RHE and N2 supply. (C1) with a potential of -0.2 V vs RHE and Ar supply. (C2) using blank GDE with a potential of -0.2 V vs RHE and N2 supply. (C3) with a open circle potential and N2 supply.

Figure S18.  Quantifying the ammonia production of 4 wt. % Mo/C-N-21 operated in a flow cell for 10 hours by NMR with 15N labelling.

Figure S19. SEM images of as-fabricated GDE with different catalyst loading: a) Blank GDL, b) 0.5 mg∙cm-2, c) 1 mg∙cm-2, d) 1.5 mg∙cm-2, e) 2 mg∙cm-2, f) 2.5 mg∙cm-2.

Figure S20. Faradaic efficiencies and NH3 yield rate of 4 wt. % Mo-PNC-21 in GDE with different catalyst loading.

Figure S21. a) Digital photos of the contact angle of as-fabricated GDE with a catalyst loading of 2 mg∙cm-2 and with different PTFE loading. b) Summary of applied PTFE loading vs. detected contact angles.

Figure S22. Faradaic efficiencies and NH3 yield rate of 4 wt. % Mo-PNC-21 in GDE with different PTFE amount.

Figure S23. Nyquist plots of 4 wt. % Mo/N-C-21 recorded in N2 condition with different applied potentials.

Table S2. Calculated resistance values based on equivalent circle.

| Sample | Average Pore Size (nm) | Rs (Ω) | Rct/Rp(Ω) | Rct (Ω) |
| --- | --- | --- | --- | --- |
| 4 wt. % Mo-PNC-8 | 8 | 1.8 | 52.2 | 21.8 |
| 4 wt. % Mo-PNC-15 | 15 | 1.8 | 52.6 | 22.4 |
| 4 wt. % Mo-PNC-21 | 21 | 1.8 | 53.2 | 23.0 |
| 4 wt. % Mo-PNC-33 | 33 | 1.8 | 52.8 | 27.6 |
| 4 wt. % Mo-PNC-56 | 56 | 1.8 | 52.4 | 30.6 |

a)

b)

Figure S24. Comparison of experimental values and XGBoost model predictions for a) Faradaic efficiency and b) NH3 yield.

Figure S25. I-t curve obtained by 4 wt. % Mo/C-N-21 in optimized GDE condition for 10 hours eNRR experiment at -0.2 V vs. RHE.

Figure S26. SEM images of 4 wt. % Mo/C-N-21 in optimized GDE condition before (a,c) and  after (b,d) 10 hours eNRR at -0.2 V vs. RHE.

Figure S27. XPS analysis of 4 wt. % Mo/C-N-21 in optimized GDE condition after 10 hours eNRR at -0.2 V vs. RHE.

Table S3. Summary of prior studies on electrochemical NH3 synthesis.

| Catalysts | Electrolyte | Potential (vs. RHE) | NH3 Yield Rate (μg∙h-1∙mg-1) | FE [%] | References |
| --- | --- | --- | --- | --- | --- |
| Mo-PNC | 0.1 M KOH | -0.2 V | 34.7 | 21.6 | This work |
| VN NPs | 0.05 M H2SO4 | -0.1 V | 20.2 | 6 | J. Am. Chem. Soc. 2018, 140, 13387. |
| Cr2O3 | 0.1 M Na2SO4 | -0.9 V | 3.04 | 6.78 | ACS Catal. 2018, 8, 8540. |
| C@CoS@TiO2 | 0.1 M Na2SO4 | -0.55 V | 49.51 | 28.6 | Angew. Chem., Int. Ed. 2019, 58, 18903. |
| GDY/Co2N | 0.1 M HCl | -0.2 V | 219.72 | 58.6 | Angew. Chem., Int. Ed. 2020, 59, 13021. |
| Fe–Ni LDH | 0.1 M Na2SO4 | -0.5 V | 10.53 | 23 | Angew. Chem., Int. Ed. 2020, 59, 13623. |
| Cu/PI-300 | 0.1 M KOH | -0.3 V | 12.4 | 6.56 | Nat. Commun. 2019, 10, 4380. |
| Cu-TiO2/CP | 0.5 M LiClO4 | -0.55 V | 21.31 | 21.99 | Adv. Mater. 2020, 32, 2000299. |
| Nb2O5 nanofiber | 0.1 M HCl | -0.55 V | 43.6 | 9.26 | Nano Energy 2018, 52, 264. |
| 2D W2N3 | 0.1 M KOH | -0.2 V | 11.66 | 11.67 | Adv. Mater. 2019, 31, 1902709. |
| PC/Sb/SbPO4 | 0.1 M HCl | -0.25 V | 25 | 31 | Angew. Chem., Int. Ed. 2019, 58, 13329. |
| Sc/NC | 0.1 M HCl | -0.1 V | 20.4 | 11.2 | ACS Nano 2020, 14, 1093. |
| Y/NC | 0.1 M HCl | -0.1 V | 23.2 | 12.1 | ACS Nano 2020, 14, 1093. |
| Re2MnS6 | 0.1 M Na2SO4 | -0.3 V | 15 | 14 | Nano Lett. 2020, 20, 4960. |
| Fe-ReS2 | 0.1 M Na2SO4 | -0.2 V | 80.4 | 12.3 | Adv. Funct. Mater. 2020, 30, 1907376. |
| THH Au NRs | 0.1 M KOH | -0.2 | 1.648 | 4.02 | Adv. Mater. 2017, 29, 1604799. |
| Vr-ReSe2@CBC | 0.1 M Na2SO4 | -0.25 | 28.3 | 42.5 | Angew. Chem., Int. Ed. 2020, 59, 13320. |
| Ru SAs/N-C | 0.05 M H2SO4 | -0.2 | 120.9 | 29.6 | Adv. Mater. 2018, 30, 1803498. |
| Ru@ZrO2/NC | 0.1 M HCl | -0.11 | 3600 | 21 | Chem 2019, 5, 204. |
| Ru SAs/g-C3N4 | 0.05 M NaOH | 0.05 | 23 | 8.3 | Adv. Funct. Mater. 2020, 30, 1905665. |
| Pd/C | 0.05 M H2SO4 | 0.1 | 4.5 | 8.2 | Nat. Commun. 2018, 9, 1795. |
| PdH0.43 | 0.1 M PBS | -0.15 | 20.4 | 43.6 | Angew. Chem., Int. Ed. 2020, 59, 3511. |
| PdPb nanosponges | 0.1 M HCl | 0.05 | 25.68 | 5.79 | Appl. Catal., B 2020, 265, 118481 |
| Pd0.2Cu0.8/rGO | 0.1 M KOH | -0.2 | 2.8 | 0.6 | Adv. Energy Mater. 2018, 8, 1800124. |
| PdCu/NC | 0.05 M H2SO4 | -0.45 | 69.2 | 24.8 | Angew. Chem., Int. Ed. 2020, 133, 349. |
| NPG@ZIF-8 | 0.1 M Na2SO4 | -0.8 | 28.7 | 44 | Angew. Chem., Int. Ed. 2019, 58, 15362. |
| AuHNCs | 0.5 M LiClO4 | -0.4 | 3.9 | 30.2 | Nano Energy 2018, 49, 316. |
| Au/TiO2 | 0.1 M HCl | -0.2 | 21.4 | 8.11 | Adv. Mater. 2017, 29, 1606550. |
| α-Au/CeOx-RGO | 0.1 M HCl | -0.2 | 8.3 | 10.1 | Adv. Mater. 2017, 29, 1700001. |
| Au6/Ni | 0.05 M H2SO4 | -0.14 | 7.4 | 67.8 | J. Am. Chem. Soc. 2019, 141, 14976. |
| Au/CoOx | 0.05 M H2SO4 | -0.5 | 15.1 | 19 | Angew. Chem., Int. Ed. 2019, 58, 18604. |
| ISAS-Fe/NC | 0.1 M PBS | -0.4 | 62.9 | 18.6 | Nano Energy 2019, 61, 420. |
| Fe SA-N-C | 0.1 M KOH | 0 | 7.48 | 56.55 | Nat. Commun. 2019, 10, 341. |
| Fe-N/C | 0.1 M KOH | -0.2 | 34.83 | 9.28 | ACS Catal. 2019, 9, 336. |
| FePc/C | 0.1 M Na2SO4 | -0.3 | 137.95 | 10.5 | ACS Catal. 2019, 9, 7311. |
| Mo3Fe3C | 0.1 M Li2SO4 | -0.05 | 1.23 | 27 | Nano Energy 2020, 68, 10437. |
| SA-Mo/NPC | 0.1 M KOH | -0.3 | 34 | 14.6 | Angew. Chem., Int. Ed. 2019, 58, 2321. |
| Mo0/GDY | 0.1 M HCl | -0.1V | 2 | 15.6 | J. Am. Chem. Soc. 2019, 141, 10677. |
| MoS2/CC | 0.1 M Na2SO4 | -0.5 | 4.96 | 1.17 | Adv. Mater. 2018, 30, 1800191. |
| DR MoS2/CPE | 0.1 M Na2SO4 | -0.4 | 29.28 | 8.34 | Adv. Energy Mater. 2018, 8, 1801357. |
| Co-doped MoS2-x | 0.01 M H2SO4 | -0.3 | 10.2 | 10 | J. Am. Chem. Soc. 2019, 141, 19269. |
| Ti3C2Tx (TO, OH) | 0.1 M HCl | -0.3 | 36.9 | 9.1 | ACS Energy Lett. 2019, 4, 1053. |
| MXene/TiFeOx-700 | 0.05 M H2SO4 | -0.2 | 21.9 | 25.44 | ACS Nano 2020, 14, 9089. |
| TiO2/Ti3C2Tx | 0.1 M HCl | -0.55 | 32.17 | 16.07 | Adv. Energy Mater. 2019, 9, 1803406. |
| Zr-TiO2 | 0.1 M KOH | -0.45 | 8.9 | 17.3 | Nat. Commun. 2019, 10, 2877. |
| Bi NS | 0.1 M Na2SO4 | -0.8 | 13.23 | 10.46 | ACS Catal. 2019, 9, 2902. |
| BiNCs with K+ | 0.5 M K2SO4 | -0.6 | 884 | 66 | Nat. Catal. 2019, 2, 448. |
| PEBCD with Li+ | 0.5 M Li2SO4 | -0.7 | 2.01 | 2.85 | J. Am. Chem. Soc. 2017, 139, 9771. |
| PCN-NVx | 0.1 M Na2SO4 | -0.2 | 8.09 | 11.59 | Angew. Chem., Int. Ed. 2018, 57, 10246. |
| NPC | 0.05 M H2SO4 | -0.9 | 23.8 | 1.42 | ACS Catal. 2018, 8, 1186. |
| C-ZIF | 0.1 M KOH | -0.3 | 57.8 | 10.2 | Nano Energy 2018, 48, 217. |
| CNS | 0.25 M LiClO4 | -1.19 | 97.18 | 11.56 | Sci. Adv. 2018, 4, e1700336. |
| BG | 0.05 M H2SO4 | -0.5 | 9.8 | 10.8 | Joule 2018, 2, 1610. |
| B-BCN | 0.05 M Na2SO4 | -0.6 | 8.39 | 9.87 | Appl. Catal., B 2021, 283, 119622. |
| BNS | 0.1 M Na2SO4 | -0.8 | 13.22 | 4.04 | ACS Catal. 2019, 9, 4609. |
| FL-BP NSs | 0.01 M HCl | -0.7 | 31.37 | 5.07 | Angew. Chem., Int. Ed. 2019, 58, 2612. |

Figure S28. a) Plots of Faradaic efficiencies and NH3 yield rates summarized in table S1 and recent reports of flow cells.

Figure S29. (a) Current density and Faradaic efficiencies of flow cell with 4 wt. % Mo/N-C-21 GDE under DC voltage.  (b) V-I curve and calculated power density, in which scatter line represents the actually power density for ammonia production.